## Slide 1
TPgui – Calibration tool for the MSU ISV Thermoplastic (TP) Model, v.1.2
TPgui Web
Service
Material Properties Repository
J.L. Bouvard
R.L. Carino
(Ongoing work)
Plotting routine, model calibration routine (MATLAB)
Stand-alone
TPgui (MATLAB)
TP model
(MATLAB)
Notes: TP model – model code
Model calibration wrapper – implements the logic for model calibration
Stand-alone TPgui – for users on Windows/Linux desktops/laptops that may not have a network connection
(future) TPgui web service – for users on the WWW
Material Properties Repository – a component of the CAVS-CMD CyberInfrastructure which stores experimental data, models, and model calibration tools

## Slide 2
Optimized
model constants
Good
fit ?
Yes
Generate candidate constants
No
TP model
Model stress-
strain
props()
Optimizer
Experimental stress-strain
Initial model constants
Model calibration in TPgui
User inputs

## Slide 3: TPgui strategy
Update the GUI regions in the ff. order:
Datasets
Loading parameters
Solution settings
Fixed constants
Viscoelasticity
Time dependence
Strain hardening 1
Strain softening
Strain hardening 2
A
B
C
E
H
F
G
D
I

## Slide 4: Dataset – a text file containing name= value
#
# Data set for MSU ThermoPlastic Model v.1.2
#
model_tag= TP
# Fields in the data set
# Material (or material) - Tag for material
# Expt tag (or tag) - Tag for experiment
# Source (or source) - Source of data set
# Comment (or comment) - Any other comment on data set
# Test type (or dstype) - 1=Uniaxial 2=Shear 3=Cyclic 4=Relaxation 5=Time relaxation 6=Softening 7=Yield peak 8=Visco-elasticity
# Units (or units) - Stress units: 1=psi 2=Ksi 3=Pa 4=KPa 5=MPa 6=GPa
# Tinit (or temp) - Temperature
# Rate (or e_dot) - Strain rate
# t_hold (or hold_time) - Hold time
# e_res - Residual strain
# Nstep - No. of strain levels for relaxation
# Ncyc - No. of cycles
# e_max - Max of Strain
# excluded - Is dataset excluded? 0=no, 1=yes
# experiment – experimental values
#
(continued)
(continuation)
#
material= PC
tag= PC1-cyc_0.001_RT
source= default
comment= Cyclic data at 0.001/s
dstype= 3
units= 5
temp= 298
e_dot= -0.001
hold_time= 0
e_res= 0
Nstep= 0
Ncyc= 1
e_max= 1
excluded= 0
time= 0
# Experimental data
experiment=
0 0
0.00378683 8.09759
0.00757367 16.1952
0.0113605 24.2507
0.0151473 32.2601
0.0189342 39.8368
0.022721 46.6583
…

## Slide 5: Typical sequence of steps
Load all experimental datasets. For each dataset, establish the experiment settings (initial temperature, strain rate, stress units, etc), loading parameters, and fixed constants.
First fit the datasets for two different strain rates at a reference temperature. If there are different tests, fit the compression datasets first, followed by tension datasets.

## Slide 6: Typical sequence of steps (cont)
For the first datasets, adjust the parameter groups as follows:
Viscoelasticity
Time dependence
Strain hardening 1
Strain softening
Strain hardening 2

## Slide 7: Typical sequence of steps (cont)
Restore second dataset (or other datasets available for the same temperature).

## Slide 8: Typical sequence of steps (cont)
5. Fit the parameters for different temperatures
Viscoelasticity
Time dependence
Strain hardening 1
Strain softening
Strain hardening 2

## Slide 9: Typical sequence of steps (cont)
6. Repeat step 4 for the rest of the datasets. Adjust compression and tension datasets using constants and C4, if adding stress state dependent experimental data.

## Slide 10: Typical sequence of steps (cont)
7. Record results (“Output”)
  - Write a postprocessing info text file
  - Write a restart file
  - Write a data file
  - Write a “parameters+constaints” file
  - Print figure

## Slide 11: Parametric study on the material constitutive behavior
Time dependence

## Slide 12: Parametric study on the material constitutive behavior (cont)
Strain hardening 1

## Slide 13: Parametric study on the material constitutive behavior (cont)
Strain softening

## Slide 14: Parametric study on the material constitutive behavior (cont)
Strain hardening 2

## Slide 15: Polycarbonate (PC) example
Datasets
PC1: Polycarbonate, 298K, -0.001/s, Cyclic Compression
PC2: Polycarbonate, 298K, -0.1/s, Cyclic Compression
PC3: Polycarbonate, 298K, -1500/s, Compression
PC4: Polycarbonate, 253K, -0.001/s, Cyclic Compression
PC5: Polycarbonate, 373K, -0.001/s, Cyclic Compression
PC6: Polycarbonate, 373K, -0.01/s, Cyclic Compression
PC7: Polycarbonate, 298K, 0.001/s, Tension
PC8: Polycarbonate, 298K, 0.1/s, Tension

## Slide 16: Typical sequence of steps
Load all experimental datasets. For each dataset, establish the experiment settings (initial temperature, strain rate, stress units, etc), loading parameters, and fixed constants.
…

## Slide 17: Input | A data file
Select all datasets

## Slide 18: After input of ‘Compression’ datasets
Input other datasets:
‘Tension’
‘Viscoelasticity’
‘YieldPeak’

## Slide 19: After input of all datasets

## Slide 20: Enable model plots

## Slide 21: After enabling model plots

## Slide 22: Hide plot legends

## Slide 23: After hiding plot legends

## Slide 24: Typical sequence of steps …
First fit the datasets for two different strain rates at a reference temperature. If there are different tests, fit the compression datasets first, followed by tension datasets.
For the first datasets, adjust the parameter groups as follows:
  Viscoelasticity
  …

## Slide 25: Exclude all datasets except PC1, PC2, Viscoelasticity

## Slide 26: PC1, PC2, Viscoelasticity datasets
Modulus calculated from compression tests at different strain rates at 298K

## Slide 27: Restore plot legends

## Slide 28: Step 3
For the first datasets, adjust the constants groups as follows:
Viscoelasticity
Time dependence
Strain hardening 1
Strain softening
Strain hardening 2
For a large variety of thermoplastics

## Slide 29: Elasticity: Eref=2250; “Apply”
For many thermoplastics,

## Slide 30: Step 3
For the first datasets, adjust the constants groups as follows:
Viscoelasticity
Time dependence
Strain hardening 1
Strain softening
Strain hardening 2
For a large variety of thermoplastics

## Slide 31: Exclude “Viscoelasticity”, include “Yield Peak”

## Slide 32: “Parameter Study” γv0=7.5E18, in [1.5E10,1.0E25]
Right-click to activate
Parameter Study

## Slide 33: “Parameter Study” V=5E-29, in [0,1E-20]
Right-click to activate
Parameter Study

## Slide 34: “Parameter Study” m=7, in [0,100]
Right-click to activate
Parameter Study

## Slide 35: “Parameter Study” C4=39, in [0,100]
Right-click to activate
Parameter Study

## Slide 36: “Optimize parameters” - C3
Uncheck
“Use lsqnonlin”
Use defaults

## Slide 37: Step 3
For the first datasets, adjust the constants groups as follows:
Viscoelasticity
Time dependence
Strain hardening 1
Strain softening
Strain hardening 2
For a large variety of thermoplastics

## Slide 38: Exclude PC2 & Peak Yield datasets

## Slide 39: “Parameter Study” C2=20, in [10,30]
Right-click

## Slide 40: “Parameter Study” C4=20, in [10,30]
Right-click

## Slide 41: “Parameter Study” lL=4, C14=0.99

## Slide 42: Step 3
For the first datasets, adjust the constants groups as follows:
Viscoelasticity
Time dependence
Strain hardening 1
Strain softening
Strain hardening 2
For a large variety of thermoplastics

## Slide 43: “Parameter Study” ak1=0.05, in [0.01,0.1]

## Slide 44: “Parameter Study” C10=6, in [3,8]

## Slide 45: Optimize C4, C6, and C8

## Slide 46: Step 3
For the first datasets, adjust the constants groups as follows:
Viscoelasticity
Time dependence
Strain hardening 1
Strain softening
Strain hardening 2
For a large variety of thermoplastics

## Slide 47: “Parameter Study” ak2=0.05, in [0.01,0.1]

## Slide 48: “Parameter Study” h1=2, C12=0.6

## Slide 49: Step 3
Repeat step 3 (c-e) to adjust compression data by using optimization technique

## Slide 50: Optimize C4, C2, C6, C8, and C10

## Slide 51: Step 4
Restore second dataset (or other datasets available for the same temperature).

## Slide 52: Restore PC2
Right-click
Left-click

## Slide 53: Restore PC3
Right-click
Left-click

## Slide 54: Step 3
For the first datasets, adjust the constants groups as follows:
Viscoelasticity
Time dependence
Strain hardening 1
Strain softening
Strain hardening 2
For a large variety of thermoplastics
Optimization

## Slide 55: “Optimize” C4, lL , C2, h0, C6, C8, C10, h1, C12

## Slide 56: Step 5
5. Fit the parameters for different temperatures
Viscoelasticity
Time dependence
Strain hardening 1
Strain softening
Strain hardening 2

## Slide 57: Exclude PC2, PC3; Restore PC4, PC5

## Slide 58: Step 5
5. Fit the parameters for different temperatures
Viscoelasticity
  E1=-1.5, in [-10,0]
Time dependence
Strain hardening 1
  C1=-0.05, in [-1,0]
Strain softening
  C7=0; C5=-0.0001, C9=-0.001, in [-1,0]
Strain hardening 2
  “Parameter Study” C11=-0.001, in [-1,0]

## Slide 59: Step 5
5. Fit the parameter for different temperatures
Viscoelasticity
Time dependence
Strain hardening 1
Strain softening
Strain hardening 2

## Slide 60: “Parameter Study” E1=-1.5, in [-10,0]

## Slide 61: Step 5
5. Fit the parameter for different temperatures
Viscoelasticity
Time dependence
Strain hardening 1
Strain softening
Strain hardening 2

## Slide 62: Time dependence: C3, C4

## Slide 63: “Parameter Study” C1=-0.05 in [-1;0]

## Slide 64: “Optimize” C1
Optimization not successful; try another method

## Slide 65: “Parameter Study” C5=-0.0001 and C9=-0.001

## Slide 66: “Parameter Study” C11=-0.001, in [-0.5,0]

## Slide 67: Step 6
6. Repeat step 4 for the rest of the datasets. Adjust compression and tension datasets using constants p and C4, if adding stress state dependent experimental data.

## Slide 68: Restore PC7, PC8
Right-click
Right-click

## Slide 69: “Parameter Study” p =0.19 in [0;1] (p can be chosen using values from the literature)

## Slide 70: Optimize, by lsqnonlin: C3, C4, C1, C2, h0, C5, C6, C8, C9, C10, h1, C11, C12

## Slide 71: Step 7
Record results (“Output”)
  - Write a postprocessing info text file
  - Write a restart file
  - Write a data file
  - Write a “parameters+constaints” file
  - Print figure

## Slide 72: Write a record of the fitting session